Technical Data Sheet

| Revision Date | 24 October 2018 |
| --- | --- |
| Multisorb Part Number | Product Name | Description |
| 02-00832AG08 | NatraSorb® Bulk Molecular Sieve | Bulk Molecular Sieve 13X |

MATERIALS OF CONSTRUCTION

| Components | Molecular Sieve 13X Bead 8 x 12 Mesh |
| --- | --- |

PHYSICAL ATTRIBUTES

| Attribute | Specification | Comments |
| --- | --- | --- |
| Sorbent Weight | 30.0 +1.0 / -0.0 lbs (13.61 +0.45 / -0.00 kg) | 30.0 - 31.0 lbs (13.61 - 14.06kg) |
| Moisture Content | 2% Maximum | Product is quality released using residual moisture testing per Multisorb Loss on Drying Test Method (10-20 grams at 427°C ( 15°C for 3 hours Minimum). |

PACKAGING, LABELING, PRODUCT STORAGE, AND WARRANTY PERIOD

| Attribute | Specification |
| --- | --- |
| Quantity | Packed 30 lbs per 5 gallon steel pail. |
| Labeling | Manufacturer’s CAUTION label on the lid. |
|  | Manufacturer’s name, description of desiccant, weight per container, part number, and batch number. |
| Product Storage | Recommended storage in a non-condensing environment. Avoid temperatures above 32ºC (90ºF). |
| Warranty Period | Product meets specified physical attributes for a period of 1 year from date of manufacture when stored in original unopened packaging. |

# Text boxes

EXCEPT TO THE EXTENT REQUIRED BY STATE LAW, SELLER EXPRESSLY DISCLAIMS ALL WARRANTIES, EXPRESSED OR IMPLIED, INCLUDING ANY IMPLIED WARRANTY OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE.