Technical Data Sheet

| Revision Date | 09 January 2019 |
| --- | --- |
| Multisorb Part Number | Product Name | Description |
| 02-00630AG08 | NatraSorb® Bulk Indicating Silica Gel | Bulk Indicating Silica Gel |

MATERIALS OF CONSTRUCTION

| Components | Indicating Silica Gel Bead 4 x 12 Mesh |
| --- | --- |

PHYSICAL ATTRIBUTES

| Attribute | Specification | Comments |
| --- | --- | --- |
| Sorbent Weight | 60.0 (1.5 lbs (27.21 (0.68 kg) | 58.5 - 61.5 lbs (26.53 - 27.89 kg) |
| Moisture Content | 4.0% Maximum | Product is quality released using residual moisture testing per Multisorb Loss on Drying Test Method (10-20 grams at 150°C ( 15°C for 3 hours Minimum). |

PACKAGING, LABELING, PRODUCT STORAGE, AND WARRANTY PERIOD

| Attribute | Specification |
| --- | --- |
| Quantity | Packed 60 lbs per 10 gallon fiber drum with polyliner and twist tie. |
| Labeling | Manufacturer’s CAUTION label on the lid. |
|  | Manufacturer’s name, description of desiccant, weight per container, part number, and batch number. |
| Product Storage | Recommended storage in a non-condensing environment. Avoid temperatures above 32ºC (90ºF). |
| Warranty Period | Product meets specified physical attributes for a period of 1 year from date of manufacture when stored in original unopened packaging. |

# Text boxes

EXCEPT TO THE EXTENT REQUIRED BY STATE LAW, SELLER EXPRESSLY DISCLAIMS ALL WARRANTIES, EXPRESSED OR IMPLIED, INCLUDING ANY IMPLIED WARRANTY OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE.