Technical Data Sheet

| Revision Date |  | 24 October 2018 |  |
| --- | --- | --- | --- |
| Multisorb Part Number | Product Name |  | Description |
| 02-00630AG27 | NatraSorb® Bulk Silica Gel |  | Bulk Silica Gel, 0.5-1.5 mm |

MATERIALS OF CONSTRUCTION

| Components | Silica Gel Granular 4 x 12 Mesh |
| --- | --- |

PHYSICAL ATTRIBUTES

| Attribute | Specification | Comments |
| --- | --- | --- |
| Sorbent Weight | 30.0  1.5 lbs (13.61  0.68 kg) | 28.5 – 31.5 lbs (12.93 – 14.29kg) |
| Moisture Content | 2% Maximum | Product is quality released using residual moisture testing per Multisorb Loss on Drying Test Method (10-20 grams at 150°C  15°C for 3 hours Minimum). |

PACKAGING, LABELING, PRODUCT STORAGE, AND WARRANTY PERIOD

| Attribute | Specification |
| --- | --- |
| Quantity | Packed 30 lbs per 5 gallon steel pail. |
| Labeling | Manufacturer’s CAUTION label on the lid. |
|  | Manufacturer’s name, description of desiccant, weight per container, part number, and batch number. |
| Product Storage | Recommended storage in a non-condensing environment. Avoid temperatures above 32ºC (90ºF). |
| Warranty Period | Product meets specified physical attributes for a period of 1 year from date of manufacture when stored in original unopened packaging. |

EXCEPT TO THE EXTENT REQUIRED BY STATE LAW, SELLER EXPRESSLY DISCLAIMS ALL WARRANTIES, EXPRESSED OR IMPLIED, INCLUDING ANY IMPLIED WARRANTY OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE.