Technical Data Sheet

| Revision Date |  | 20 November 2018 |  |
| --- | --- | --- | --- |
| Multisorb Part Number | Product Name |  | Description |
| 07-66X16BG10 | Bulk Indicating Silica Gel |  | Type A, Blue Indicating Silica Gel, 1.5-3.0 mm |

MATERIALS OF CONSTRUCTION

| Components | 1.5-3.0 mm, Blue, Indicating Type A Silica Gel |
| --- | --- |

PHYSICAL ATTRIBUTES

| Attribute | Specification |  | Comments |
| --- | --- | --- | --- |
| Sorbent Weight | 1.50-1.55 lbs (680-703 gms) |  | N/A |
| Moisture Content | 2% Maximum |  | Product is quality released using residual moisture testing per Multisorb Loss on Drying Test Method (10-20 grams at 150°C  15°C for 3 hours Minimum). |
| Particle Size Distribution (U.S. Std. Sieve) | On 6 mesh Thru 18 mesh | 2.0 max 5.0 max | N/A |
| Typical Minimum Adsorption Capacity | % By Weight 8 13 20 | @ RH & 25°C 20 35 50 | Product is not quality released using adsorption capacity testing. |
| Typical Minimum Bulk Density | 45 lbs/ft3 (720 g/L) |  | N/A |

PACKAGING, LABELING, PRODUCT STORAGE, AND WARRANTY PERIOD

| Attribute | Specification |
| --- | --- |
| Quantity | Packed 1.5 lbs per 1 quart can and 12 cans per carton. |
| Labeling | Manufacturer’s CAUTION statement printed on carton. |
|  | Manufacturer’s name, description of desiccant, weight per container, part number, and batch number. |
| Product Storage | Recommended storage in a non-condensing environment. Avoid temperatures above 32ºC (90ºF). |
| Warranty Period | Product meets specified physical attributes for a period of 1 year from date of manufacture when stored in original unopened packaging. |

EXCEPT TO THE EXTENT REQUIRED BY STATE LAW, SELLER EXPRESSLY DISCLAIMS ALL WARRANTIES, EXPRESSED OR IMPLIED, INCLUDING ANY IMPLIED WARRANTY OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE.